## Slide 1
12.10.2023, Hotel Palisad, Zlatibor,
CCM 2023
Advances in understanding of technologies for treatment of critical minerals
Srecko Stopic, Christian Dertmann, Bernd Friedrich

## Slide 2: Critical Minerals
Mineral | Chemical composition in ore
Bastnäsit | (Ce, La, Y)CO3F
Monazit | (Ce,La,Nd,Th)PO4
Xenotim | YPO4
Eudialyt | Na15Ca6(Fe,Mn)3Zr3SiO(O,OH,H2O)3 (Si3O9)2(Si9O27)2(OH,Cl)2
Fosters Lake
Grönland

## Slide 3: Generic REE conceptual flowsheet
N. Verbaan et al. (2015)
A review of hydrometallurgical flowsheets considered in REE.
Current projects
Symposium on critical and strategic materials
British Colombia Geological Survey paper

## Slide 4: Benefication Process

## Slide 5: Chemical composition of eudialyte ore, Grönland
Elements | Si | Al | Fe | Ca | Na | K | Ti | Mn | Nb | Zr | TREE
wt.% | 23.1 | 3.2 | 6.0 | 5.7 | 9.9 | 0.8 | 0.2 | 0.3 | 0.1 | 6.5 | 1.6
Chart: 
| Ce | Dy | Eu | Er | Gd | La | Lu | Nd | Pr | Sm | Tb | Tm | Y | Yb | Ho
 | 32.7203 | 3.2967 | 2.1731 | 0.24077 | 2.63 | 18.3357 | 0.29695 | 13.0264 | 3.7474 | 2.6485 | 0.48093 | 0.35745 | 17.1627 | 2.1484 | 0.73466
Eudialyte is a Na-rich zirconosilicate with constant amount of elements including REE.
Na15Ca6Fe3Zr3Si(Si25O75)(O,OH,H2O)3(Cl,OH)3

## Slide 6: About the EURARE Program

## Slide 7: Demonstration plant for production of rare earth carbonate
Variable | Minimum | Mean | Maximum
Concentrate: HCl/ (kg/L) | 1: 1 | 1: 1.25 | 1: 1.5
Concentrate: Water/ (kg/L) | 1: 1 | 1: 2 | 1: 3
Leaching Temperature/ ℃ | 20 | 50 | 80
Reaction time/ min | 20 | 40 | 60
Y.Ma, S.Stopic, B.Friedrich,
Hydrometallurgical Treatment of a Eudialyte Concentrate for Preparation of Rare Earth Carbonate, Johnson Matthey Technology Review, January 2019, 8
Y. Ma, S.Stopic, L.Gronen, S.Obradovic, M.Milivojevic, B.Friedrich, Neural Network Modeling
for the Extraction of Rare Earth Elements from Eudialyte Concentrate by
Dry Digestion and Leaching, Metals, 2018, 8 (4), 267

## Slide 8: Initial IME/MEAB Strategy for REE ore treatment

## Slide 9: Dry digestion process (fuming) - the heart of this process
Characteristics:
Average treatment rate (kg/hour): 6
Reactor volume (L): 40
Digestion media HCl, 31% (L): 6-7.2
Washing media H2O (L): 18-24
Dry digestion time (min): 45
Washing time (min): 15
Temperature: 20°C, due to exothermic effect increase to 60-70 °C
Flux- air operated diafragm pump
Flow rate (30 L/min)
Operated pressure

## Slide 10: pH adjustment using CaCO3 (Norra Kärr-Sweden and Tanbarez-Grönland)
At pH 4 (first stage of leach purification), mainly Fe transferred to the residue, while REEs remain in solution

## Slide 11: Filtration using a semi-continuous chamber filter press
pH of solution smaller than 4.0-4.1
Max pressure: 6 bar
Flow rate of suspension: 1-1.2 L/min

## Slide 12: REE precipitation efficiency with Na2CO3
Chart: Elements
| La | Ce | Y | Nd | Gd | Zr | Si | Fe | Al
 | 98.5982 | 98.8123 | 95.0407 | 99.1953 | 97.4227 | 80.7692 | 0 | 77.2285 | 97.709
After precipitation with sodium carbonate, more than 95 % of REEs transferred to REE-carbonate

## Slide 13: Removal of iron from the produced REE-Carbonate
REE carbonate re-dissolved with HCl
With NaOH a second precipitation was performed
Oxidation of Fe(II) to Fe(III) using 4 ml 30 % H2O2/1 L solution
pH value adjusted using diluted NaOH to pH 3.5 to 3.8
Need of flocculants, filtration

## Slide 14: Produced REE carbonate (31 % REE)
 | La | Ce | Nd | Tb | Gd | Y | Sm | Dy | Eu
 | % | % | % | % | % | % | % | % | %
REE carbonate | 5,23 | 10,5 | 3,90 | 0,20 | 0,85 | 7,15 | 0,93 | 1,17 | 0,08
 | He | Sc | Fe | Al | Zr | Na | Ca | Mn | Si
 | % | % | % | % | % | % | % | % | %
REE carbonate | 0,78 | <0,01 | 0,20 | 3,31 | 0,05 | 4.43 | 4,18 | 0,23 | 0.03

## Slide 15: Recovery of rare earth elements from eudialyte, nickel lateritic ore and red mud
Duration: 01.04.2019-31.12.2021, ZIM AIF- Financial support, Germany (MAREKO Project)
Title: Development of a modular reactor for the dry digestion of high silicon-rich ores and concentrates to avoid gel formation using the example of eudialyte concentrates
Konsortium: IME, RWTH Aachen, Germany and Konzept GmbH, Germany
filterable silica coagulate
D. Vosenkaul, B.Friedrich,..
J. Sustain. Metall. (2017) 3:79–89
MeSiO3 + H2O + 2 HCl = Si(OH)4 + MeCl2

## Slide 16: Development of Dry digestion reactor for dissolution of ores
2L reactor
(Maximal charging- 1 kg)
40L Reactor (EURARE)
(maximal charging 10 kg)
Improvement:
Countercurrent flow mixing system
Separated acid and water injection
Large volume
Higher ore charging
Corrosion resistance materials

## Slide 17: Dry digestion reactor, konzept GmbH, Germany
Characteristics of reactor:
Volumen (L): 100
Weight of solid (kg): 40
Manual injection of solid materials
Nozzle system for water and acid injection
Countercurrent flow mixing system
No heating in reactor
High concentration of acid (<10 mol/L) enables a strong exothermic reaction
After the mixing process, the leached product leaves the mixing chamber through the outlet flaps
With permission of Konzept, Düren, Germany

## Slide 18: Chemical composition of studied materials with reaction parameters
Al | Fe | Ti | Ca | Si | Zr | Mn | La | Ce | Y | Nd
% | % | % | % | % | % | % | ppm | Ppm | ppm | ppm
8,92 | 3,62 | 0,13 | 1,59 | 25,1 | 0,77 | 0,14 | 554 | 1400 | 897 | 650
.
Al | Fe | Ti | Ca | Si | Sc | V | Ce | Y
% | % | % | % | % | ppm | ppm | Ppm | ppm
13,90 | 6,14 | 4,47 | 9,29 | 18,1 | 108 | ´429 | 462 | 124
Al | Fe | Ti | Cr | Si | Ni | V | Sc | Y
% | % | % | % | % | % | ppm | ppm | ppm
1,13 | 29,80 | 0,02 | 0,57 | 16,7 | 1,68 | 61 | 47 | 4
Eudialyte
Bauxite residue
Lateritic oxidic ores
Parameter | Unit | Value
Initial Material | kg | 20
Used acid | - | 96% H2SO4
concentration | mol/l | 12
Duration of dry digestion | min | 120
Solid /liquid in dry digestion (H2SO4) | - | 1:2
Solid/liquid in leaching (H2O) | - | 1:5
Duration of leaching | min | 60
Main aims:
High leaching efficiency of REE
Avoiding of the silica gel formation

## Slide 19: Dry digestion of Eudialyte and Bauxite residue
Chart: Eudialyte
Al | 26.1211
Fe | 9.2541
Ti | 46.7308
Mn | 57.8571
Zr | 65.2597
La | 100.1805
Ce | 99.6429
Y | 96.1538
Nd | 91.1538
Si | 0.20179
High leaching efficiency for La, Ce, Nd and Y higher than 90 %.
Chart: Bauxite Residue
Al | 43.3967
Fe | 19.8675
Ti | 40.7649
Mn | 94.0278
Zr | 44.1883
La | 94.1489
Ce | 81.129
Y | 101.25
Nd | 65.3947
Sc | 71.3235
Si | 1.5682
High leaching efficiency for Y and La and Mn

## Slide 20: Dry digestion of the nickel lateric ore from Turkey
Sample | Eudialyte | Red Mud | Ni-Laterite
Initial mass (kg) | 20,00 | 20,00 | 20,00
Si in initial mass (g) | 5020,00 | 770,00 | 3338,26
CSi in Solution (mg/L) | 101,3 | 120,75 | 31,75
Si in solution (g) | 10,13 | 12,08 | 3,18
Efficiency (%) | 0,20 | 1,57 | 0,10
Chart: Metallausbeute in %
Al | 43.5128
Fe | 15.6455
Ti | 130.7371
Cr | 11.1804
Ni | 52.0346
V | 59.8361
Sc | 44.6809
Si | 0.095109
High leaching efficiency for Ti (about 100 %), 60 % V, 50 % Ni, 45 % Sc and minimal dissolution of silicon.

## Slide 21: EURO-TITAN (01.01.2024-31.12.2027)
Hydrogen-Plasma reduction of industrial wastes
Technical University Clausthal, Germany (Coordinator)
Other Participants:
RWTH-Aachen
ALUMINA, Zvornik
Technological Faculty, Zvornik
Private companies from Greece, Germany, France)

## Slide 22: Summary
Future development in rare earth metallurgy needs the new raw materials, applications, and technology.
Processing of ores produces the concentrates with different content of rare earths.
The most used minerals in production of rare earths: Bastnäsite, Xenotime, Eudialyte, Monazite.
The applied hydrometallurgical processes (leaching, filtration and precipitation) result in the production of rare earth carbonate.
After the thermal cracking of rare earth carbonate, the rare earth oxide were produced
Technical innovations are changing demand behavior and causing commodity markets to become unbalanced.

## Slide 23
sstopic@ime-aachen.de